## "Table of modern battery sizes" (c) GFDL by Wikipedia editors, http://en.wikipedia.org/wiki/Battery_sizes#Table_of_modern_battery_sizes Retrieved March 16, 2008,

## Table of battery sizes

| Most Common Name | Other Common Names | IEC Name | ANSI/NEDA Name | Typical Capacity (mAh) | Nominal Voltage | Shape | Terminal layout | Dimensions | Comments |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 123 | Camera Battery CR123 | CR17354 (Lithium) | 5018LC (Lithium) | 1500 (Lithium) 700 (Li-Ion) | 3 | Cylinder | + Nub cylinder end - Flat opposite end | L 34.5 mm D 17 mm | 123 always implies lithium chemistry |
| 4.5 Volt | Bardic Lamp Battery Pocketable Battery 1203 4.5 V | 3LR12 (alkaline) 3R12 (carbon-zinc) | MN1203 (manganese) | 2500 (alkaline) 1200 (carbon-zinc) | 4.5 (always) | Flat pack | + short terminal strip - long terminal strip | H 70 mm L 60 mm W 22 mm | May be replaced by 3 AA cells using a plastic stub enclosure (not practical) |
| 9 Volt | PP3 9-Volt Radio battery | 6LR61 (alkaline) 6F22 (carbon-zinc) 6KR61 (NiCd) | 1604A (alkaline) 1604D (carbon-zinc) 1604LC (Lithium) 11604 (NiCd) 7.2H5 (NiMH) | 565 (alkaline) 400 (carbon-zinc) 1200 (lithium) 120 (NiCd) 175 (NiMH) 500 (Lithium polymer rechrg) | 9 7.2 (NiCd) 7.2 (NiMH) 8.4 (some NiCd and NiMH) | Rectangular | both small end + male clasp - female clasp | H 48.5 mm L 26.5 mm W 17.5 mm | Many (not all) 9v batteries are an array of 6 reversed-polarity (nub is negative while can is positive) AAAA batteries welded together internally |
| A23 | 23A 3LR50 | 3LR50 (alkaline) | 1181A (alkaline) | 40 (alkaline) | 12 | Cylinder (or button stack) | + Nub cylinder end - Flat opposite end | L 29 mm D 10 mm | Used in small RF devices such as key fob-style garage door openers and keyless entry systems where only infrequent pulse current is used. Sometimes enclosed like a normal battery but sometimes a stack of 8 LR(?) button cells shrink wrapped together. (see here about naming) |
| AA | Penlight Mignon | LR6 (alkaline) R6 (carbon-zinc) FR6 (Lithium-FeS2) KR157/51 (NiCd) | 15A (alkaline) 15D (carbon-zinc) 15LF (Lithium-FeS2) 10015 (NiCd) 1.2H2 (NiMH) | 2700 (alkaline) 1100 (carbon-zinc) 3000 (Lithium-FeS2) 600-1000 (NiCd) 1700-2900 (NiMH) | 1.5 1.2 (NiCd) 1.2 (NiMH) | Cylinder | + Nub cylinder end - Flat opposite end | L 50.5 mm D 13.5-14.5 mm | C7/HP7; |
| AAA | Microlight Potlood | LR03 (alkaline) R03 (carbon-zinc) | 24A (alkaline) 24D (carbon-zinc) | 1200 (alkaline) 540 (carbon-zinc) 800-1000 (Ni-MH) | 1.5 1.2 (NiCd) 1.2 (NiMH) | Cylinder | + Nub cylinder end - Flat opposite end | L 44.5 mm D 10.5 mm | C16/HP16; |
| AAAA |  | LR8D425 (alkaline) | 25A (alkaline) | 625 (alkaline) | 1.5 | Cylinder | + Nub cylinder end - Flat opposite end | L 42.5 mm D 8.3 mm | Obscure type sometimes used in 'pen flashlights' or electronic glucose meters. Most common use is as an internal component of 9v batteries. |
| C | Mignon | LR14 (alkaline) R14 (carbon-zinc) | 14A (alkaline) 14D (carbon-zinc) | 8000 (alkaline) 3800 (carbon-zinc) | 1.5 | Cylinder | + Nub cylinder end - Flat opposite end | L 50 mm D 26.2 mm | C11/SP11/HP11; Can be replaced with alkaline AA cell using plastic sabot (stub case) |
| See naming notes below about CR battery types |
| CR927 |  |  |  | 30 (Lithium) | 3 | Coin | + bottom/sides - top | D 9.5 mm H 2.7 mm | This obscure type of lithium coin cell is used extensively in blinkies. |
| CR1220 |  | CR1220 (Lithium) |  | 40 (Lithium) | 3 | Coin | + bottom/sides - top | D 12.5 mm H 2.0 mm | Standard Discharge Current: 0.1 mA. |
| CR1225 |  | CR1225 (Lithium) |  | 50 (Lithium) | 3 | Coin | + bottom/sides - top | D 12.5 mm H 2.5 mm | Standart discharge current: 0.2 mA. Maximum discharge current: 1 mA. Maximum pulse discharge current: 5 mA. |
| CR1620 |  | CR1620 (Lithium) |  | 78 (Lithium) | 3 | Coin | + bottom/sides - top | D 16 mm H 2.0 mm | Standard Discharge Current: 0.1 mA. |
| CR2016 |  | CR2016 (Lithium) | 5000LC (Lithium) | 90 (Lithium) | 3 | Coin | + bottom/sides - top | D 20 mm H 1.6 mm | Standard Discharge Current: 0.1 mA. Often used in pairs instead of CR2032 for devices that require more than 3 volts, like blue/white LED flashlights. CAUTION: Using 2 CR2016 when not specified can damage a device. |
| CR2025 |  | CR2025 (Lithium) | ? (Lithium) | 160 (Lithium) | 3 | Coin | + bottom/sides - top | D 20 mm H 2.5 mm | Standard Discharge Current: 0.2 mA. |
| CR2032 |  | CR2032 (Lithium) | 5004LC (Lithium) | 225 (Lithium) | 3 | Coin | + bottom/sides - top | D 20 mm H 3.2 mm | Standard Discharge Current: 0.2 mA. Maximum discharge current: 3 mA. Maximum pulse discharge current: 15 mA. Common battery in computers to keep the date and CMOS settings current when power is off. |
| CR2450 |  | CR2450 (Lithium) | 5029LC (Lithium) | 610 (Lithium) | 3 | Coin | + bottom/sides - top | D 24.5 mm H 5.0 mm | Portable devices requiring high current (30 mA) and long shelf life (up to 10 years) |
| D | Goliath Flashlight Battery | LR20 (alkaline) R20 (carbon-zinc) | 13A (alkaline) 13D (carbon-zinc) | 19500 (alkaline) 8000 (carbon-zinc) | 1.5 | Cylinder | + Nub cylinder end - Flat opposite end | L 61.5 mm D 34.2 mm | C2/SP2/HP2; Can be replaced with alkaline AA cell using plastic sabot (stub case) |
| J |  | 4LR61 (alkaline) | 1412A (alkaline) | 625 (alkaline) | 6 | Square with missing corner | Flat contacts - top side + missing corner | H 48.5 mm L 35.6 mm W 9.18 mm | Typically used in applications where the device in question needs to be flat, or where the battery should be unable to be put in reverse polarity--such as a blood glucose meter or blood pressure cuff. Also good for elderly persons, due to the large size. |
| Lantern (Spring) | Lantern 6 Volt Spring Top | 4R25Y (alkaline) 4R25 (carbon-zinc) | 908A (alkaline) 908D (carbon-zinc) | 26000 (alkaline) 10500 (carbon-zinc) | 6 | Square | Springs Top + Corner - Center | H 115 mm L 68.2 mm W 68.2 mm | Springs are usually made so that leads for screw top can be fastened to them. In most applications this is fine (see next). |
| Lantern (Screw) | Lantern 6 Volt Screw Top | 4R25Y (alkaline) 4R25 (carbon-zinc) | 915A (alkaline) 908 (carbon-zinc) | 26000 (alkaline) 10500 (carbon-zinc) | 6 | Square | Screw Posts Top + Corner - Center | H 115 mm L 68.2 mm W 68.2 mm | For uses that have high vibration/shock where the leads may be knocked off of springs. |
| Lantern (Big) | 918 R25-2 Big Lantern Double Lantern | 4LR25-24 (alkaline) 4R25-2 (carbon-zinc) 8R25 (carbon-zinc) | 918A (alkaline) 918D (carbon-zinc) | 52000 (alkaline) 22000 (carbon-zinc) | 6 | Square | Screw posts Apart top | H 127 mm L 136.5 mm W 73 mm |  |
| N | Lady | LR1 (alkaline) | 910A (alkaline) | 1000 (alkaline) | 1.5 | Cylinder | + Nub cylinder end - Flat opposite end | L 30.2 mm D 12 mm | Typical uses include remote-control door chimes, and other low current drain devices. Also used for wireless microphones, and "Mr. Microphone" type devices. |
| See Naming Notes below about SR/LR battery types |
| SR41 | AG3 LR41 | LR41 (alkaline) SR41 (silver-oxide) | 1135SO (silver-oxide) 1134SO (silver-oxide) | 32 (alkaline) 42 (silver-oxide) | 1.50 (alkaline) 1.55 (silver-oxide) | Button | + bottom/sides - top | D 7.9 mm H 3.6 mm |  |
| SR43 | AG12 LR43 | LR43 (alkaline) SR43 (silver-oxide) | 1133SO (silver-oxide) 1132SO (silver-oxide) | 80 (alkaline) 120 (silver-oxide) | 1.50 (alkaline) 1.55 (silver-oxide) | Button | + bottom/sides - top | D 11.6 mm H 4.2 mm |  |
| SR44 | AG13 LR44 | LR44 (alkaline) SR44 (silver-oxide) | 1166A (alkaline) 1107SO (silver-oxide) 1131SOP (silver-oxide) | 150 (alkaline) 200 (silver-oxide) | 1.50 (alkaline) 1.55 (silver-oxide) | Button | + bottom/sides - top | D 11.6 mm H 5.4 mm |  |
| SR48 | AG5 | SR48 (silver-oxide) | 1136SO (silver-oxide) 1137SO (silver-oxide) | 70 (silver-oxide) | 1.55 (silver-oxide) | Button | + bottom/sides - top | D 7.9 mm H 5.4 mm |  |
| SR54 | AG10 LR54 | LR54 (alkaline) SR54 (silver-oxide) | 1138SO (silver-oxide) | 100 (alkaline) 85? (silver-oxide) | 1.50 (alkaline) 1.55 (silver-oxide) | Button | + bottom/sides - top | D 11.6 mm H 3.1 mm |  |
| SR57 |  | LR57&nbsp(alkaline) SR57 (silver-oxide) | 116550 (silver-oxide) | 55 (silver-oxide) | 1.55 (silver-oxide) | Button | + bottom/sides - top | D 9.4 mm H 2.8 mm |  |
| SR60 | AG1 | SR60 (silver-oxide) | 1175SO (silver-oxide) | 20 (silver-oxide) | 1.55 (silver-oxide) | Button | + bottom/sides - top | D 6.8 mm H 2.15 mm |  |
| SR66 | AG4 | SR66 (silver-oxide) | 1176SO (silver-oxide) | 26 (silver-oxide) | 1.55 (silver-oxide) | Button | + bottom/sides - top | D 6.8 mm H 2.6 mm |  |